[image: image1.png]


Primary Lithium Battery
ER34615T
3.6V Li/SOCL2 System Battery Size D, High-energy Battery
[image: image12.png]E

%0

20

T2
BE(C)

ry





Advantages:
●   stable high VOP and Capacitance
● High Energy Density and stable current
● Wide working temperature range(-55℃~+85℃)
● Lower Self discharge rate(EVG annual rate below under +20℃ surroundings)
● Excellent environment application features
● Stainless steel shells(Low magnetism and environment erosion resistance)
Features：
●  Positive poles with independent proprietary technology
●    Stainless steel-Glass hermetic package
●    Non combustible electrolyte
●    High short circuit safety
●    Meet the technical requirements of IEC60086.4:2014
● Passed UL component testing certification（MH45919）
●Comply with RoHS environmental requirements ， easy to be recycled.
Main application
Utility meters
Alarms and safety equipments
Memory storage backup devices
RFID
Automotive electronics
Real time clocks
Marine surveying equipment Oil production equipment


	Electrical Performance

	(Typical data from those being stored for or within 12 months under 25±5℃ surroundings)
Normal Capacity：                                             19.0Ah
（The capacity is tested under the condition of 2.0mA ，+25℃ and cutoff voltage 2.0V.Battery capacity will change with the change of discharge current,ambient tempreture and cutoff voltage.）

	Open circuit voltage  Typical data at+25℃ :
	3.67V

	Nominal voltage（at +25℃with load 0.2mA）：
	3.60V


Maximum continuous discharge current                                                                                    230mA
（If you need higher current than that of 50% normal capacity at +25℃ and 2.0V cutoff voltage, pls contact manufacture     )
 SHAPE  \* MERGEFORMAT 



(At+25℃, An unused battery begin to discharge with 10μA base current, and during the process, a pulse of 400mA/0. 1s will be discharged every two minutes,when the voltage reading will be higher than 3.0v. The voltage reading will change with  the change of the pulse characters,temperatures and store conditions. If under hard conditions, we suggest using LICC or SC together with batteries. Details pls contact manufacture  )。
	Storage（ Suggestion）                                                                        +30℃  at most

(If you have higher requirements or harsh terms, pls contact manufacture )

	Operating temperature range                                                -55℃-+85℃
(If exceeded, capacity will decrease, voltage reading be too lower and Initial pulse voltage reading be relatively low. )

	Physical Performance

	Diameter（Max）
	34.5mm

	Height（Max）
	61.5mm

	Typical weight
	101 g

	Lithium metal content
	about    5. 1g


[image: image10.png]


Warning：Do not charge,short circuit,heat over 100℃ 、 breakdown 、put into water、or weld directly on the surface of the shells. If you do like that, explosion, burning or Acid leakage inside the battery will be caused.
[image: image3.png]



[image: image11.png]


Primary Lithium Battery
ER34615T
3.6V Li/SOCL2 System Battery Size D, High-energy Battery
[image: image4.png]



[image: image5.jpg]Max®342




Size unit:mm（unmarked tolerance base on the standard of GB1804-m） If extreme connection mold needed, we can make to order. Pls contact
manufacture 
Warning
● No short circuit
● No charge
● No puncturing
● No pressing
● Be sure to connect anode and cathode with the equipments correctly.
● No disassembling
● No burning
● No using old and new batteries simultaneously
● No heating over 100℃
● No welding batteries directly
● No transforming or modifying
Notice：manufacture  has the rights to information covered by changes to this documentation without notice first. Any specifications involved in    this documentation is only for your reference. Only by written
confirmation between supply and demand parties can the content in this file be used as valid information of the contract.


1.Typical discharge curve at +25℃（ Median）
[image: image6.png](V)

19}

1ol

10100 100 1000

Biakh)

100000




2 Voltage curve under different current and tempreture（Stable discharge process
3.Capacity curve under different tempreture and current (cutoff voltage 2.0V)
[image: image7.jpg]AR (mA)




4.Storage Character
[image: image8.jpg]RENV)

10|

20

MM 20mA  BE25T

EOCTHE0ORE | wk
(REFESCTFRION)

T 00

st

7,000




[image: image9.png]









Maximum pulse capacity current                                                                                                    400mA















